## Slide 1
NLL 83 %
WATER-COOLED
BAFFLES (4)
M
M-101
JI
100
XS
101
R-101
PVC SUSPENSION POLYMERISATION REACTOR
140 m3, D 4.5 m x T/T 7.4 m
15.2 barg & FV / 93 C, JACKET 5.2 barg
AGITATOR M-101 330 kW, 2 IMPELLERS
D-105
SHORT-STOP POT
N2-PRESSURISED
S
XV-104
FC
1"-SS-104
D-104
INITIATOR
DOSING POT
P-104
S
XV-103
FC
1"-IN-103
VCM FROM
TK-100 (25 C)
P-103
FIC
102
FV-102
FC
FQ 51 t
S
XV-102
FC
4"-VC-102
DEMIN WATER
55 C, 6 barg
TK-107 PVA
HV-107
FIC
101
FQ 60 t
FV-101
FC
S
XV-101
FC
6"-PW-101
INJECTION WATER
30 C, 16 barg
FIC
103
FV-103
FC
SP FROM LIC-100 (CAS)
2"-PW-103
TO VCM
RECOVERY
6"-VG-105
PSV-100
SET 15.0 barg
TO DUMP TANK D-103
S
XV-108
FC (ESD)
TO EMERG. VENT TANK
S
XV-109
FC
TO VACUUM PUMP VP-101
S
XV-105
FC
PV-105 (HIC-105)
FC
PCV-141 1.5 barg
HV-141
N2 PAD
6 barg
18"-VG-110 VCM VAPOUR UP / CONDENSATE DOWN
PI
100
PT
101
PSHH-101
12.5 barg
HV-135 (HIC-135)
FC
TI
132
CWR TO TE-131 (PID-002)
CWS FROM FV-130 (PID-002)
E-101
REFLUX CONDENSER
VERTICAL, VCM IN TUBES
LIC
100
LSHH
100
LT-100 RADAR; SP TO FIC-103
JACKET RETURN TO P-101A/B (PID-002)
BAFFLE CWR TO TE-121 (PID-002)
BAFFLE CWS FROM FV-120 (PID-002)
JACKET SUPPLY FROM TE-110 (PID-002)
10"-CW-111
10"-CW-110
TIC
100
TT
101
TSHH-101 63 C
(INDEPENDENT TE)
SP TO TIC-110
(PID-002)
XI-100
CALC.
CALORIMETRIC
CONVERSION
WI
100
LOAD CELLS (3), CONTENTS t
S
XV-106
FC
PVC SLURRY TO BLOWDOWN TANK D-102
8"-SL-106
LEGEND
PROCESS LINE
UTILITY LINE (CW, STEAM, N2)
SIGNAL LINE
LINE JUMP (NO JOIN)
CONTROL VALVE FO / FC
ON/OFF VALVE (SEQ. / SIS)
MANUAL VALVE
ORIFICE FLOW ELEMENT
TI
DCS INSTRUMENT
TI
FIELD INSTRUMENT
TI
SIS FUNCTION
DCS FUNCTION BLOCK
OFF-SHEET LINK
RELIEF VALVE
CONTROL LOOP SCHEDULE
LOOP
MEASURES
MOVES
FAIL
SET / NOTE
FIC-101
WATER CHARGE
FV-101
FC
240 m3/h, FQ 60 t
FIC-102
VCM CHARGE
FV-102
FC
180 t/h, FQ 51 t
LIC-100
R-101 LEVEL
FIC-103 SP
-
83 %
FIC-103
INJECTION WATER
FV-103
FC
CAS (~3 m3/h)
TIC-100
R-101 TEMP.
TIC-110 SP
-
57.0 C (K 67)
TIC-110
JACKET INLET
TY-110
-
CAS (~38 C)
TY-110
0-50 % OUT
TV-110A STEAM
FC
HEAT-UP
TY-110
50-100 % OUT
TV-110B CW
FO
COOLING
FIC-120
BAFFLE CW
FV-120
FO
80 m3/h
VPC-130
TIC-110 OUT
FIC-130 SP
-
50 % (NOTE 5)
FIC-130
E-101 CW
FV-130
FO
CAS
HIC-135
-
HV-135 INERTS
FC
MANUAL
HIC-105
-
PV-105 DEGAS
FC
END OF BATCH
SIS INTERLOCKS
I-
INITIATOR
SETTING
ACTION
1
TSHH-101 R-101 TEMP.
> 63 C, 10 s
A
2
PSHH-101 R-101 PRESS.
> 12.5 barg, 5 s
A
3
XS-101 AGITATOR STOP
REACTING, 15 s
A
4
FSLL-110 JACKET FLOW
< 120 m3/h, 30 s
A
5
LSHH-100 R-101 LEVEL
> 94 %, 5 s
B
6
HS-001 ESD PUSHBUTTON
MANUAL
A + XV-108
A = SHORT-STOP XV-104, CLOSE XV-101/102/103, FV-103 TO 0,
FORCE TV-110B / FV-120 / FV-130 OPEN. B = CLOSE XV-101/102, FV-103.
ITEM (OTS DESIGN POINT)
VALUE
WATER / VCM CHARGE
60 t (55 C) / 51 t (25 C)
REACTION
57.0 C, 8.6 barg
LEVEL / CONTENTS AT 2 h
83 % / 117.8 t
Q REACTION AT 2 h
2.71 MW (PEAK 3.43)
JACKET / BAFFLES / E-101
1.48 / 0.40 / 0.98 MW
END POINT
dP 1.8 bar, X 0.85
PVC PER BATCH / TIME
43.2 t / 5.3 h
GENERAL NOTES:
1. DESIGN BASIS (REFERENCE CARD): VINYL CHLORIDE IN WATER -> PVC; JACKETED BATCH TANK + REFLUX CONDENSER; 50-70 C, 8-12 bar; ORGANIC PEROXIDE INITIATOR; 200 kt/y -> 7.9 MW (dHp 71 kJ/mol, 8000 h/y). PLANT = 4 x 140 m3 REACTORS R-101..R-104; THIS SHEET = R-101 (OTS UNIT).
2. RECIPE (ASSUMED OTS DESIGN POINT): 60 t DEMIN WATER 55 C + PVA (HV-107), 51 t VCM, INITIATORS A + B (t1/2 1.5 h / 12 h AT 57 C), 57.0 C (GRADE K 67). END POINT = PRESSURE DROP 1.8 bar -> 85 % CONVERSION, 43.2 t PVC, REACTION 5.3 h; CYCLE ~7 h -> 4 x 43.2 t x 8000 / 6.9 h = 200 kt/y.
3. VESSEL D 4.5 m x T/T 7.4 m (141.5 m3), SS-CLAD. SHELL 15.2 barg & FULL VACUUM / 93 C, JACKET 5.2 barg (220 / 75 psi, 200 F). PSV-100 SET 15.0 barg TO DUMP TANK D-103: RUNAWAY / TWO-PHASE RELIEF SIZING TBC (DIERS METHOD).
4. BATCH SEQUENCE (DCS): XV-109 EVACUATE TO <= 0.05 bar a -> XV-101 WATER (FQ PRESET) -> XV-102 VCM (PERMISSIVES: XV-106 SHUT, EVACUATED, WATER >= 95 %, M-101 RUNNING, FI-110 >= 300 m3/h) -> HEAT-UP -> XV-103 INITIATOR AT TI-100 >= 54 C -> REACTION -> END POINT
-> XV-104 SHORT-STOP -> XV-105 / PV-105 DEGAS BELOW 2 barg -> HV-141 N2 PAD (1.5 barg) -> XV-106 DISCHARGE. ALL XV FAIL CLOSED; SEQUENCE SIGNALS NOT SHOWN.
5. E-101: VCM VAPOUR UP AND CONDENSATE BACK DOWN THE SAME 18" NOZZLE. INERTS (N2 / AIR) COLLECT AT THE TOP AND BLANKET THE TUBES (TI-132 FALLS TOWARD CW TEMPERATURE) - VENT WITH HV-135. E-101 CW BY VPC-130 / FIC-130 ON PVC-PID-002 (ANTI-FOAM LIMIT 12 m3/h PER % XI-100).
6. XI-100 = CALORIMETRIC CONVERSION IN DCS = INTEGRAL(JACKET + BAFFLE + E-101 DUTIES - AGITATOR POWER + HEAT STORED) / (dHp x FQ-102).
7. LIC-100 (RADAR) HOLDS THE LEVEL WITH SHRINKAGE-COMPENSATION WATER (FIC-103 IN CASCADE): PVC 1.40 vs VCM 0.85 t/m3 -> ABOUT 20 m3 INJECTED PER BATCH; KEEPS THE JACKET WETTED.
8. SIS I-1..I-6 IN A SEPARATE LOGIC SOLVER (TABLE). SHORT-STOP POT D-105 IS N2-PRESSURISED; SHORT-STOP ONLY MIXES WITH THE AGITATOR RUNNING (< 30 s) - AGITATOR ON EMERGENCY POWER (TBC).
9. LINE SIZES AND MATERIALS PRELIMINARY - TBC BY PIPING. SERVICE CODES: PW PROCESS WATER, VC VCM LIQUID, VG VCM GAS, IN INITIATOR, SS SHORT-STOP, SL SLURRY, NG NITROGEN, CW COOLING / JACKET WATER.
REV
DESCRIPTION
DATE
A
ISSUED FOR OTS DEVELOPMENT (REVIEW)
25-SEP-26
CHULA CHEM. ENG. - PVC REACTOR VER 1 (OTS)
P&ID - R-101 PVC REACTOR,
CHARGES, CONDENSER, VENTS
DRAWN: APINAN
SOOTTITANTAWAT
CHK'D: --
APP'D: --
DATE: 25-SEP-26
DWG NO.
PVC-PID-001
REV
A
SCALE
N.T.S.
SHEET
1 OF 2