## Slide 1
TK-100
VCM Storage
P-103
VCM Charge Pump
TK-107
PVA Pot
D-104
Initiator Pot
(chilled)
P-104
Initiator Dosing
Pump
D-105
Short-stop Pot
(N2)
R-101
PVC Reactor 140
m3
E-101
Reflux Condenser
VP-101
Vacuum Pump
D-103
Emergency Vent
Tank
D-106
VCM Gasholder
1.25 bar a
C-101
VCM Recovery
Compressor
P-101 A/B
Jacket
Circulation
Pumps
D-102
Blowdown /
Slurry Tank
P-102
Slurry Pump
T-201
Slurry Stripping
Column
S-201
Dewatering
Centrifuge
D-201
PVC Dryer
PVC SUSPENSION REACTOR VER 1 · OPERATOR TRAINING SIMULATOR
PFD-100 PVC suspension polymerisation — R-101 area
PVC SUSPENSION POLYMERISATION — R-101 AREA (1 OF 4 REACTORS)
DRAWING No.
PFD-100
REV.
0
SIZE
A4
SHEET
1 OF 1
DRAWN
Apinan Soottitantawat
CHECKED
SCALE
NTS
DATE
2026-09-29
LEGEND
Mass Flow (t/h)
Liquid Flow (m³/h)
Temperature (°C)
Pressure (bar g)
Process Line
Utility Line
Block Valve
Control Valve
Process Input / Output
Stream Number
Line Crossing
Vessel / Drum
Centrifugal Pump
PD Pump
Stirred Reactor
Heat Exchanger
Blower / Fan
Storage Tank
NOTES
1. Flags: R-101 design state 2.0 h into the reaction (OTS model); charge rates are the FIC set points.
2. Batch: 60 t water + PVA, 51 t VCM, initiator; 57 °C, 8.6 bar g; end point at 1.8 bar pressure drop.
3. Recovered VCM is condensed before storage (condenser not shown). Baffle CW and N2 pad not shown.
4. T-201, S-201, D-201 are shared by R-101 to R-104 and shown as blocks only.
1
2
3
180
25
12
4
5
6
240
55
5
7
8
9
10
12.9
57
8.6
11
12
13
14
15
0.24
16
17
18
19
20
21
22
468
38.2
23
24
25
26
27
28
29
30
TK-100
P-103
TK-107
D-104
P-104
D-105
R-101
E-101
cw
VP-101
D-103
D-106
C-101
P-101 A/B
D-102
P-102
T-201
S-201
D-201
VCM from Unloading
Demin Water 55 °C
Nitrogen
Vent Gas to Treatment
CW
LP Steam
PVC Powder
Mother Liquor to WWT
Reflux
Recovered VCM
Stripped VCM